## Slide 1
Three-Dimensional Reconstruction of Nb3Sn Thin Films
Eric Viklund1,2, David Seidman1, Jae-yel Lee2, Sam Posen2
1Northwestern University, 2Fermi National Accelerator Laboratory
Introduction
Nb3Sn SRF cavities manufactured using Sn-vapor deposition are a promising candidate for future accelerator applications to achieve higher Q and higher accelerating gradients.
Sn-deficient regions are formed during the growth of the Nb3Sn film.
Sn deficient regions theorized to form during nucleation.
Sn predominantly diffuses through Nb3Sn grain boundaries (GBs).
Sn cannot reach the center of grains due to slow intra-granular diffusion.
Figure 1: TEM-EDS image showing Sn-deficient regions near the Nb-Nb3Sn interface.1
Figure 4: The orientation of the sample, ion-beam, and electron-beam during a FIB tomography measurement.
Jaeyel Lee et al 2019 Supercond. Sci. Technol. 32 024001
Focused Ion-Beam Tomography
Sources
e-
Ga+
Figure 2: The mechanism which generates Sn-deficient regions during the vapor-diffusion coating process.1
In this study we use 3D EDS and EBSD methods to image the distribution of Sn-depleted regions in Nb3Sn films and correlate their position with grains and grain boundaries.
We find several areas where the film is thin or Sn deficient, which could contribute to poor cavity performance.
EBSD measurements indicate that the Sn deficient regions are located within the Nb3Sn grains as is predicted by our Nb3Sn nucleation model.
Conclusion
Figure 5: The orientation of the sample, ion-beam, and electron-beam during a FIB tomography measurement. A thin region of the film and a Sn-deficient region have been indicated by a red circle.
Figure 3: The boundaries of the Nb3Sn film calculated from the 3-D Sn X-ray count distribution. The threshold value for the iso-surface was chosen as 1.5x106.
Figure 6: Volume rendering of the 3-dimensional Sn X-ray count data.
Combined focused ion beam and electron beam instrument at FNAL allows for 3D characterization of Nb3Sn films.
Combining EDS measurements with EBSD gives a clearer picture.
Thin regions form between grain boundaries.
Sn deficient regions form within the grains.
This suggests that our model of Sn deficient region formation is correct.
Combined EDS and EBSD Measurements
Figure 7: Simultaneous measurement of grain orientation and Sn content of a Nb3Sn film.
Sn deficient regions found throughout the film.
Film fails to grow in some regions leading to thin areas.
Acknowledgement
This manuscript has been authored by Fermi Research Alliance, LLC under Contract No. DE-AC02-07CH11359 with the U.S. Department of Energy, Office of Science, Office of High Energy Physics.